## Slide 1
Lucas Brouwer, Mariusz Juchno, Diego Arbelaez, Paolo Ferracin (for the CCT Team)
6/15/2021
CCT6 preliminary analysis and next steps

## Slide 2: CCT6 is a Large Aperture, 12-13 T Nb3Sn Magnet for Hybrid Testing
CCT R&D goal d) “Demonstration of bore field up to 13 T in a 120-mm aperture in a four-layer Nb3Sn CCT model magnet”

## Slide 3: Outline
Initial Analysis Goals – outline for this talk
short-sample field vs. cable size at 4.5 K and 1.9 K
preliminary cable selection and 2D cross section
2D mechanical analysis with a rigid boundary
initial steps towards 3D modeling

## Slide 4: CCT6 Initial Design Assumptions
Assumptions
120 mm clear bore diameter
four layers
insulation and channel design is based on CCT5
Jc = 3000 A/mm^2 @4.2 K, 12 T
cable
ins. + gap of 300 μ per side

## Slide 5: A 2D magnetic model is used for scaling studies
Assumptions
10” of iron close to the outer coil
5% rise of field at conductor due to 3D effects not captured by this model*
3 mm spar + 1 mm radial gap between layers
short-sample is with respect to round wire Jc
This model allows for quick study of short-sample fields attainable for a variety of cables
*based on past 4+ CCT layer designs

## Slide 6: Short-Sample vs. Cable Width for 0.85 mm strand
Assumptions for scaling study: 0.85 mm strand, non-cu fraction of 0.46
Choice of a large cable (20-25 mm) targets 12 T at 4.5 K and 13 T at 1.9 K ( at 80% of SSL)

## Slide 7: Explore CCT6 design using existing LD1 cable
Ref. P. Ferracin et al., IEEE TASC 22(2), 2012

## Slide 8: Four layers with LD1 cable leads to 12 T at 4.5 K and 13 T at 1.9 K (at 80% of SSL)
Four Layers @ SSL
 | 4.5 K | 1.9 K
current | 15.0 kA | 16.8 kA
B_cond | 15.8 T | 17.5 T
B_bore | 15.0 T | 16.6 T
Four Layers @ 80 % of SSL
 | 4.5 K | 1.9 K
current | 12.0 kA | 13.4 kA
B_cond | 12.6 T | 14.0 T
B_bore | 12.0 T | 13.3 T

## Slide 9: Coil physical length to magnetic straight-section length is important for testing HTS inserts
dipole
b3
b7
b5

## Slide 10: Stored Energy and Conductor Use for LD1 Cable (51 strands)
stored energy is 5.1 MJ/m (15.0 kA: 4.5 K short-sample)
Layer | tilt angle (deg) | turns | cable length (m) | strand length (km)
1 | 18 | 100 | 106 | 5.4
2 | 18 | 100 | 144 | 7.3
3 | 25 | 150 | 211 | 10.7
4 | 25 | 150 | 255 | 13.0
without grading, requires ~720 m of cable and ~36 km of strand

## Slide 11: ANSYS model for stress estimation with an idealized structure
CCT layers with perfect sliding contact and “shims” extended to 90 degrees
Artificially stiff shell
Pre-compression applied using fixed radial displacement on outside of the shell
Load steps (2D - plane stress)
  apply fixed radial displacement on rigid shell
  apply Lorentz forces at ~80% of 4.5 K short-sample
    four layers: 12.0 kA, 12.0 T bore field
Study the case of pre-compression up to the point of no conductor azimuthal tension during powering (all Lorentz force induced tension shifted into compression)

## Slide 12: A rigid boundary with pre-stress gives a 2D estimate of peak conductor azimuthal stress of order 120 MPa
boundary is brought in 0.14 mm to keep coil barely in compression at 12.0 kA, 12.0 T bore field
after prestress
prestress+LF
Peak spar -265 MPa
Conductor +0/-120 MPa

## Slide 13: Initial steps towards 3D modeling
Pitch layer 1,2: 8.414 mm
Pitch layer 3,4: 5.679 mm

## Slide 14: Initial steps towards 3D modeling

## Slide 15: Future Work to Complete the Design of CCT6
Initial optimization of structure (keys, shim angle, etc.)
HTS Insert coupling (SSL, structure, quench protection)
First study of de-bonding
To be studied through prototyping
feasibility of machining deep channels
winding demonstration with wide cable
reaction gap needed at pole
To be studied through modeling
seven-turn wind and reaction test mandrel
2D models
3D models
3D normal and shear at cable channel interface
de-bonding with 3D shear
Final, 3D optimization of structure