## Slide 1: Update on Costheta cross section
V. Marinozzi
07/13/2021

## Slide 2: Critical current
Jc in SC obtained by scaling Jc engineering from Paolo slides
Still using linear approximation in the peak field zone
Jc for Nb3Sn: 1928 A/mm2 @16 T, 1.9 K
Jc for Bi2212: 2944 A/mm2 @20 T, 1.9 K

## Slide 3: Iron yoke

## Slide 4: Baseline classic costheta (size optimized): v9f
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 40 – 35 – 30
Cable width: 18.35 – 16.06 – 13.3 mm
Stabilizer/Superconductor: 3 – 3 – 1
Coil width: 100 mm
Current: 11120
Peak field: 20.51 – 16.02 – 12.69 T
Margin: 83.4 – 84.1 – 75.5 %
Jcu on LTS: 1229 A/mm2
Peak azimuthal Lorentz force: 156/145 MPa (LTS/HTS)

## Slide 5: Baseline classic costheta (HTS optimized): v11d
2 layer HTS, 4 layer LTS
Strands: 0.9/1.1/0.8 mm, 40 – 40– 40
Cable width: 20.65 –24.38 – 17.73 mm
Stabilizer/Superconductor: 3 – 1 – 1.5
Coil width: 129 mm
Current: 13610
Peak field: 20.35 – 15.96 – 11.96 T
Margin: 81.5 – 84.4 – 78.0 %
Jcu on LTS: 1128 A/mm2
Peak azimuthal Lorentz force: 105/152 MPa (LTS/HTS)

## Slide 6: SMCT-like with 5 mm rings: v12e
4 layer HTS, 2 layer LTS
Strands: 0.8 mm, 46 – 40 – 35
Cable width: 21.1 – 18.35– 15.51 mm
Stabilizer/Superconductor: 3 – 3 – 1.2
Coil width: 136 mm
Current: 11900 A
Peak field: 20.59 – 16.24 – 13.6 T
Margin: 79.9 – 80.7 – 83.1 %
Jcu on LTS: 1240 A/mm2

## Slide 7: SMCT-like with 5 mm rings: v13c
2 layer HTS, 4 layer LTS
Strands: 0.8 mm, 46 – 54 – 35
Cable width: 21.1 – 23.9– 15.51 mm
Stabilizer/Superconductor: 3 – 1 – 1.2
Coil width: 148 mm
Current: 11900 A
Peak field: 20.36 – 15.7 – 13.06 T
Margin: 75.8 – 85.3 – 78.8 %
Jcu on LTS: 1240 A/mm2

## Slide 8: Next steps
Iron: 25 mm from last turn, 250 mm thick
Field quality
Quench protection studies
Common coil, hear from Ramesh

## Slide 9: Cross sections

## Slide 10: v2

## Slide 11: v3

## Slide 12: V4

## Slide 13: v5

## Slide 14: v6

## Slide 15: v8

## Slide 16: v9

## Slide 17: v10

## Slide 18: v11