## Slide 1: Nb3Sn Scaling Parameterization An Introduction to “ESE”
Ian Pong (ipong@lbl.gov)
Jack Ekin

## Slide 2: Outline
Superconducting surface (a.k.a. critical surface)
Flux Pinning
Scaling
Parameterization
  Graphical Explanation
  Mathematical Explanation

## Slide 3: Critical Surface
Recall the three critical parameters: JC BC2 TC
The customary plot of J-B-T surface:
In addition, Nb3Sn is strain (ε) sensitive
JC is a function of (B, T, ε)
BC2 is a function of (T, ε)
TC is a function of (ε)
Figure by courtesy of Lyn Evans
Figure from SMH ed. 1
We will ignore strain for now, and return to it later.

## Slide 4: Flux Pinning
Nb3Sn is a Type II superconductor: normal zones can exist inside the superconductor as “flux lines”
In an applied field B, a current I generates a Lorentz force F in the orthogonal direction of magnitude I x B
If the flux lines move, there will be a voltage  resistance
Flux lines are immobilized (“pinned”), if pinning force FP ≥ I x B
In Nb3Sn, flux pinning is by grain boundaries (g.b.)
The g.b. pinning curve is described by

## Slide 5: Scaling
Important: scaling is possible because the pinning force curves (FP as a function of B), measured at different temperatures and strains, are shape invariant:
They can be registered into a single master scaling curve
Red: 4.2 K
Green: 8.0 K
Blue: 12.0 K
F  f
B  b
Thousands of IC can be predicted from just a few IC(B) measurements!
Ekin et al. SUST 29

## Slide 6: Power of Scaling: Extrapolation
Such scaling is highly advantageous for practical purposes
From the master scaling curve, the IC at any B, T, or ε values can be generated, iff the scaling parameters are known.
How to find the scaling parameters is the topic of next week’s seminar. Today I will show how the scaling parameters relate to each other and how they define the critical surface.
The power of scaling is in its capability of extrapolation. (Global fitting will only give interpolation.)

## Slide 7: F-B vs. f-b and the exponents p, q
Chart: B [T]
Chart: b
f (b) = bp (1-b)q
p = 0.5
q = 2
Pinning-force shape parameters
a.k.a. pinning force exponents
For g.b. pinning, defines the shape
How to get to the actual values?
b  B needs BC2
f  F needs FP max
f  F needs K
formally

## Slide 8: Temperature Dependence of the FP Curve
T [K]
Chart: B [T]
Chart: b
Chart: B
Chart: B
Chart: B
BC2 [T]
T = 0 K
T = 4.2 K
T = 10 K
T = 16 K
4.2
10
16
Nb3Sn FP curve is temperature dependent
If we plot the pinning force F against the actual field B instead, the curves at increasing temperatures will have a decreasing BC2, but the shape of the curve remains the same.
Now, if we plot the temperature on the third axis, we can see the BC2 dependence on T more clearly.

## Slide 9: B-T and the exponent v
T [K]
BC2 [T]
Chart: T [K]
Chart: T [K]
bC2
t
bC2 (t) = 1 – t v
If we plot reduced field against reduced temperature, we can see a power law relationship.
This is one of two ways to determine TC* -- the “effective flux-pinning critical temperature”
t  T needs TC
v defines the shape
temperature dependence of field: bC2(t)

## Slide 10: Temperature dependence of K
T [K]
Chart: B [T]
Chart: B
Chart: B
Chart: B
BC2 [T]
T = 0 K
T = 4.2 K
T = 10 K
T = 16 K
4.2
10
16
This is the other way to determine TC*

## Slide 11: K-T and the exponent η
Chart: T [K]
| 4.2 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
K Data | 45771.08 | 27686.32 | 9572.29 | 3567.06
 | 56910.2988 | 56530.0278 | 55773.1813 | 54739.6963 | 53470.6079 | 51994.0444 | 50332.8893 | 48507.4733 | 45711.9288 | 42232.1761 | 37561.4519 | 32665.0767 | 27683.1316 | 22755.1024 | 18018.7102 | 13608.0053 | 9650.6949 | 6264.4507 | 3551.6046 | 1590.8512 | 907.2135 | 422.1553 | 128.8266 | 8.8208 | 0
η defines the shape
In “Hybrid2” formulation, µ = η/2
temperature dependence of FP max
a.k.a. h(t)

## Slide 12: Summarizing (without strain)
FP = IC x B
Critical surface scales in F-B-T space instead of I-B-T space
In F-B space,
  p and q define the pinning curve shape
  b  B through BC2; f  F through K
In B-T space,
  v defines the shape of temperature dependence of field: bC2(t)
  t  T through TC
In K-T space,
  η defines the shape of temperature dependence of FP max: h(t)

## Slide 13: F-B-T Graphical Summary
F or K
T
B
η
v
p, q
F as a function of B
F as a function of B, T
BC2 as a function of T
K as a function of T
3D

## Slide 14: F-B-T-ε Graphical Summary
F or K
T
B
η
v
p, q
F as a function of B
F as a function of B, T
BC2 as a function of T
K as a function of T
3D
ε
BC2 as a function of ε
BC2 as a function of ε, T
TC as a function of ε
K as a function of ε
3D
K as a function of ε, T

## Slide 15: Strain - s(ε) a.k.a. bC2 (ε)
Chart: Strain component, ε0 [%]
| -1.9 | -1.8 | -1.7 | -1.6 | -1.5 | -1.4 | -1.3 | -1.2 | -1.1000000000000001 | -1 | -0.89999999999999991 | -0.8 | -0.7 | -0.60000000000000009 | -0.5 | -0.39999999999999991 | -0.30000000000000004 | -0.19999999999999996 | -0.10000000000000009 | 0 | 0.10000000000000009 | 0.20000000000000018 | 0.29999999999999982 | 0.39999999999999991 | 0.5 | 0.60000000000000009 | 0.70000000000000018 | 0.79999999999999982 | 0.89999999999999991 | 1 | 1.1000000000000001 | 1.2000000000000002 | 1.2999999999999998 | 1.4 | 1.5 | 1.6 | 1.7000000000000002 | 1.7999999999999998 | 1.9 | 2 | 2.0999999999999996 | 2.2000000000000002 | 2.2999999999999998 | 2.4000000000000004 | 2.5 | 2.5999999999999996 | 2.7
Total strain | 0.42298 | 0.44398 | 0.46575 | 0.48835 | 0.51184 | 0.53634 | 0.56199 | 0.58896 | 0.61747 | 0.64775 | 0.68001 | 0.71437 | 0.75077 | 0.78882 | 0.82761 | 0.86555 | 0.90026 | 0.9287 | 0.94751 | 0.95371 | 0.94536 | 0.9222 | 0.88574 | 0.83886 | 0.78512 | 0.72804 | 0.67056 | 0.61482 | 0.56218 | 0.51336 | 0.4686 | 0.42787 | 0.39098 | 0.35762 | 0.3275 | 0.30031 | 0.27575 | 0.25354 | 0.23346 | 0.21528 | 0.19879 | 0.18382 | 0.1702 | 0.15779 | 0.14646 | 0.13609 | 0.12657
Hydrostatic | 0.39541 | 0.40985 | 0.42374 | 0.43694 | 0.44928 | 0.46061 | 0.47076 | 0.4796 | 0.48698 | 0.49279 | 0.49693 | 0.49934 | 0.49998 | 0.49883 | 0.49592 | 0.49129 | 0.48502 | 0.47722 | 0.46799 | 0.45749 | 0.44585 | 0.43325 | 0.41984 | 0.40577 | 0.39121 | 0.3763 | 0.36118 | 0.34597 | 0.33079 | 0.31573 | 0.30087 | 0.2863 | 0.27206 | 0.25822 | 0.24479 | 0.23182 | 0.21933 | 0.20732 | 0.1958 | 0.18477 | 0.17424 | 0.16419 | 0.15461 | 0.1455 | 0.13684 | 0.12861 | 0.12081
Deviatoric | 0.027564 | 0.034134 | 0.04201 | 0.051405 | 0.062556 | 0.075729 | 0.091223 | 0.10936 | 0.1305 | 0.15497 | 0.18308 | 0.21503 | 0.25079 | 0.28999 | 0.33169 | 0.37425 | 0.41523 | 0.45148 | 0.47952 | 0.49622 | 0.49951 | 0.48896 | 0.46591 | 0.43309 | 0.39391 | 0.35174 | 0.30938 | 0.26885 | 0.2314 | 0.19763 | 0.16773 | 0.14158 | 0.11891 | 0.099409 | 0.082712 | 0.068485 | 0.056418 | 0.046229 | 0.037665 | 0.030505 | 0.024552 | 0.019631 | 0.015589 | 0.012293 | 0.0096225 | 0.0074761 | 0.005764
Chart: Strain component, ε0 [%]
| -1.9 | -1.8 | -1.7 | -1.6 | -1.5 | -1.4 | -1.3 | -1.2 | -1.1000000000000001 | -1 | -0.89999999999999991 | -0.8 | -0.7 | -0.60000000000000009 | -0.5 | -0.39999999999999991 | -0.30000000000000004 | -0.19999999999999996 | -0.10000000000000009 | 0 | 0.10000000000000009 | 0.20000000000000018 | 0.29999999999999982 | 0.39999999999999991 | 0.5 | 0.60000000000000009 | 0.70000000000000018 | 0.79999999999999982 | 0.89999999999999991
Total strain | 0.42298 | 0.44398 | 0.46575 | 0.48835 | 0.51184 | 0.53634 | 0.56199 | 0.58896 | 0.61747 | 0.64775 | 0.68001 | 0.71437 | 0.75077 | 0.78882 | 0.82761 | 0.86555 | 0.90026 | 0.9287 | 0.94751 | 0.95371 | 0.94536 | 0.9222 | 0.88574 | 0.83886 | 0.78512 | 0.72804 | 0.67056 | 0.61482 | 0.56218
Hydrostatic | 0.39541 | 0.40985 | 0.42374 | 0.43694 | 0.44928 | 0.46061 | 0.47076 | 0.4796 | 0.48698 | 0.49279 | 0.49693 | 0.49934 | 0.49998 | 0.49883 | 0.49592 | 0.49129 | 0.48502 | 0.47722 | 0.46799 | 0.45749 | 0.44585 | 0.43325 | 0.41984 | 0.40577 | 0.39121 | 0.3763 | 0.36118 | 0.34597 | 0.33079
Deviatoric | 0.027564 | 0.034134 | 0.04201 | 0.051405 | 0.062556 | 0.075729 | 0.091223 | 0.10936 | 0.1305 | 0.15497 | 0.18308 | 0.21503 | 0.25079 | 0.28999 | 0.33169 | 0.37425 | 0.41523 | 0.45148 | 0.47952 | 0.49622 | 0.49951 | 0.48896 | 0.46591 | 0.43309 | 0.39391 | 0.35174 | 0.30938 | 0.26885 | 0.2314
Chart: 
BC2* (ε0) [T]
  The strain function
  bC2 (ε) =
Note: in reality there is irreversibility
Note: * indicates it is extracted from IC measurements, a.k.a. “effective” BC2(ε).

## Slide 16: BC2* (ε)
Chart: 
BC2* (ε, 0) [T]
  The strain function
  bC2 (ε) =
BC2* (ε, T)

## Slide 18: BC2* (ε, T) = BC2* (0, 0) x bC2(ε) x bC2(t)
BC2* (ε, T) [T]
TC (ε) [K]
ε0 [%]

## Slide 19: Temperature Dependence of FP max a.k.a. h (t)
Chart: T [K]
| 4.2 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
K Data | 45771.08 | 27686.32 | 9572.29 | 3567.06
 | 56910.2988 | 56530.0278 | 55773.1813 | 54739.6963 | 53470.6079 | 51994.0444 | 50332.8893 | 48507.4733 | 45711.9288 | 42232.1761 | 37561.4519 | 32665.0767 | 27683.1316 | 22755.1024 | 18018.7102 | 13608.0053 | 9650.6949 | 6264.4507 | 3551.6046 | 1590.8512 | 907.2135 | 422.1553 | 128.8266 | 8.8208 | 0

## Slide 20: Strain Dependence of FP max a.k.a. g (ε)

## Slide 21: K (t, ε) = K (0, 0) x h (t) x g (ε)
K (0, 0)

## Slide 22: Mathematically…

## Slide 23: Conclusion
In Nb3Sn, flux pinning is predominantly by grain boundaries.
The pinning force curves (FP as a function of B), measured at different temperatures and strains, are shape invariant.
From the master scaling curve, the IC at any B, T, or ε values can be generated, iff the scaling parameters are known.
The power of scaling is in its capability of extrapolation.
Today I showed how the scaling parameters relate to each other and how they define the critical surface.

## Slide 24: Strain function choice: Exponential
We use the Exponential Scaling Law by Bordini et al. (SuST 26)
Chart: Strain component, ε0 [%]
| -1.9 | -1.8 | -1.7 | -1.6 | -1.5 | -1.4 | -1.3 | -1.2 | -1.1000000000000001 | -1 | -0.89999999999999991 | -0.8 | -0.7 | -0.60000000000000009 | -0.5 | -0.39999999999999991 | -0.30000000000000004 | -0.19999999999999996 | -0.10000000000000009 | 0 | 0.10000000000000009 | 0.20000000000000018 | 0.29999999999999982 | 0.39999999999999991 | 0.5 | 0.60000000000000009 | 0.70000000000000018 | 0.79999999999999982 | 0.89999999999999991 | 1 | 1.1000000000000001 | 1.2000000000000002 | 1.2999999999999998 | 1.4 | 1.5 | 1.6 | 1.7000000000000002 | 1.7999999999999998 | 1.9 | 2 | 2.0999999999999996 | 2.2000000000000002 | 2.2999999999999998 | 2.4000000000000004 | 2.5 | 2.5999999999999996 | 2.7
Total strain | 0.42298 | 0.44398 | 0.46575 | 0.48835 | 0.51184 | 0.53634 | 0.56199 | 0.58896 | 0.61747 | 0.64775 | 0.68001 | 0.71437 | 0.75077 | 0.78882 | 0.82761 | 0.86555 | 0.90026 | 0.9287 | 0.94751 | 0.95371 | 0.94536 | 0.9222 | 0.88574 | 0.83886 | 0.78512 | 0.72804 | 0.67056 | 0.61482 | 0.56218
Hydrostatic | 0.39541 | 0.40985 | 0.42374 | 0.43694 | 0.44928 | 0.46061 | 0.47076 | 0.4796 | 0.48698 | 0.49279 | 0.49693 | 0.49934 | 0.49998 | 0.49883 | 0.49592 | 0.49129 | 0.48502 | 0.47722 | 0.46799 | 0.45749 | 0.44585 | 0.43325 | 0.41984 | 0.40577 | 0.39121 | 0.3763 | 0.36118 | 0.34597 | 0.33079
Deviatoric | 0.027564 | 0.034134 | 0.04201 | 0.051405 | 0.062556 | 0.075729 | 0.091223 | 0.10936 | 0.1305 | 0.15497 | 0.18308 | 0.21503 | 0.25079 | 0.28999 | 0.33169 | 0.37425 | 0.41523 | 0.45148 | 0.47952 | 0.49622 | 0.49951 | 0.48896 | 0.46591 | 0.43309 | 0.39391 | 0.35174 | 0.30938 | 0.26885 | 0.2314
Simple to use
Has a theoretical basis (elastic strain energy)
Excellent extrapolation from very few data over extended strain
One fitting parameter in the axial case (C1)
  The strain function (> 0 and < 1) has two components:
    hydrostatic sD associated with the first strain invariant I1, and
    deviatoric sH with the second deviatoric strain invariant J2
  sD and sH never peak at the same strain component ε0
  (strain function always < 1, 3D strain ε never equals 0)
  The strain function is defined as:
  bC2 (ε) =
  where OR
  OR
  ε is the 3D strain, and ɛ0 the intrinsic axial applied strain
  ɛ0 ≡ Applied axial strain εa + Residual axial strain εl0
  (the strain component ε0 is in I1 and J2)
Chart: Strain component, ε0 [%]
| -1.9 | -1.8 | -1.7 | -1.6 | -1.5 | -1.4 | -1.3 | -1.2 | -1.1000000000000001 | -1 | -0.89999999999999991 | -0.8 | -0.7 | -0.60000000000000009 | -0.5 | -0.39999999999999991 | -0.30000000000000004 | -0.19999999999999996 | -0.10000000000000009 | 0 | 0.10000000000000009 | 0.20000000000000018 | 0.29999999999999982 | 0.39999999999999991 | 0.5 | 0.60000000000000009 | 0.70000000000000018 | 0.79999999999999982 | 0.89999999999999991 | 1 | 1.1000000000000001 | 1.2000000000000002 | 1.2999999999999998 | 1.4 | 1.5 | 1.6 | 1.7000000000000002 | 1.7999999999999998 | 1.9 | 2 | 2.0999999999999996 | 2.2000000000000002 | 2.2999999999999998 | 2.4000000000000004 | 2.5 | 2.5999999999999996 | 2.7
Total strain | 0.42298 | 0.44398 | 0.46575 | 0.48835 | 0.51184 | 0.53634 | 0.56199 | 0.58896 | 0.61747 | 0.64775 | 0.68001 | 0.71437 | 0.75077 | 0.78882 | 0.82761 | 0.86555 | 0.90026 | 0.9287 | 0.94751 | 0.95371 | 0.94536 | 0.9222 | 0.88574 | 0.83886 | 0.78512 | 0.72804 | 0.67056 | 0.61482 | 0.56218 | 0.51336 | 0.4686 | 0.42787 | 0.39098 | 0.35762 | 0.3275 | 0.30031 | 0.27575 | 0.25354 | 0.23346 | 0.21528 | 0.19879 | 0.18382 | 0.1702 | 0.15779 | 0.14646 | 0.13609 | 0.12657
Hydrostatic | 0.39541 | 0.40985 | 0.42374 | 0.43694 | 0.44928 | 0.46061 | 0.47076 | 0.4796 | 0.48698 | 0.49279 | 0.49693 | 0.49934 | 0.49998 | 0.49883 | 0.49592 | 0.49129 | 0.48502 | 0.47722 | 0.46799 | 0.45749 | 0.44585 | 0.43325 | 0.41984 | 0.40577 | 0.39121 | 0.3763 | 0.36118 | 0.34597 | 0.33079 | 0.31573 | 0.30087 | 0.2863 | 0.27206 | 0.25822 | 0.24479 | 0.23182 | 0.21933 | 0.20732 | 0.1958 | 0.18477 | 0.17424 | 0.16419 | 0.15461 | 0.1455 | 0.13684 | 0.12861 | 0.12081
Deviatoric | 0.027564 | 0.034134 | 0.04201 | 0.051405 | 0.062556 | 0.075729 | 0.091223 | 0.10936 | 0.1305 | 0.15497 | 0.18308 | 0.21503 | 0.25079 | 0.28999 | 0.33169 | 0.37425 | 0.41523 | 0.45148 | 0.47952 | 0.49622 | 0.49951 | 0.48896 | 0.46591 | 0.43309 | 0.39391 | 0.35174 | 0.30938 | 0.26885 | 0.2314 | 0.19763 | 0.16773 | 0.14158 | 0.11891 | 0.099409 | 0.082712 | 0.068485 | 0.056418 | 0.046229 | 0.037665 | 0.030505 | 0.024552 | 0.019631 | 0.015589 | 0.012293 | 0.0096225 | 0.0074761 | 0.005764

## Slide 25: Comparison of BC2 (ε) Extrapolation
SuST 26