## Slide 1
Ian Pong (ipong@lbl.gov)
Algirdas Baskys (abaskys@lbl.gov)
Lawrence Berkeley National Laboratory
HTS Test Facility Dipole Magnet Wire Specification Review
TFD Cable Packing Factor

## Slide 2: Development Cable Parameters
W12OL1302 – using the CERN wire CO11S20235A04U
Cable parameters (as-fabricated, before HT)
  W12OL1302A (“1302-A”): 25.9 mm wide, 1.93 mm thick (at 14 MPa by CME)
  W12OL1302B (“1302-B”): 25.9 mm wide, 1.91 mm thick (at 14 MPa by CME)
  W12OL1302C (“1302-C”): 26.1 mm wide, 1.91 mm thick (at 14 MPa by CME)

## Slide 3: Packing Factor
RW diameter: 1.1 mm
Cable thickness: 1.91 mm  when top and bottom strands are directly on top of another, thickness reduction is ~13%
  1.93 mm  ~12%
  Cf. MQXFA: ~10%
At the triplet, the packing factor is ~82%