## Slide 1
Alice Moros (amoros@lbl.gov)
Lawrence Berkeley National Laboratory
Towards Advanced Superconducting Performance:
Exploring the Microstructure of APC Nb3Sn Wires
SMP Seminar – 11th November 2021

## Slide 2: Outline
Alice Moros – SMP Seminar, 11th November 2021
Framework of the research study
Artificial Pinning Center (APC) Nb3Sn Wires
Introduction to my work
Microstructural analysis and employed techniques
Summary and outlook

## Slide 3: Aiming for the Future hadron Collider (FCC-hh)
Alice Moros – SMP Seminar, 11th November 2021
Parameter | LHC | FCC-hh
Collision energy [TeV] | 14 | 100
Dipole field [T] | 8.33 | 16
Circumference [km] | 26.7 | 97.75
Beam current [A] | 0.58 | 0.5
Synchr. rad. power [kW] | 3.6 | 2400
Jc = 1.5 kA/mm2 at 16 T & 4.2 K  Nb3Sn
High-field dipole magnets

## Slide 4: Jc Enhancement
JC ~ 1000 A/mm2
JC = 1500 A/ mm2
Jc = 1.5 kA/mm2 at 16 T & 4.2 K  Nb3Sn
Sn inhomogeneities
Grain size
Artificial defects
Jc
APC Nb3Sn wires have demonstrated their capability of meeting the FCC target and even exceeding it!
Xu, Xingchen, et al. "High critical current density in internally-oxidized Nb3Sn superconductors and its origin." Scripta Materialia 186 (2020): 317-320.
Xu, Xingchen, et al. "Ternary Nb3Sn superconductors with artificial pinning centers and high upper critical fields." Superconductor Science and Technology 32.2 (2019): 02LT01.

## Slide 5: Artificial Pinning Center (APC) Nb3Sn Wires
Alice Moros – SMP Seminar, 11th November 2021
Standard PIT sub-element
APC-PIT
sub-element
For APC:
SnO2 powder as an O source
Nb-Zr/Hf alloy
Xu, X., et al. "Refinement of Nb3Sn grain size by the generation of ZrO2 precipitates in Nb3Sn wires." Applied Physics Letters 104.8 (2014): 082602.)
Xu, Xingchen, et al. "Ternary Nb3Sn superconductors with artificial pinning centers and high upper critical fields." Superconductor Science and Technology 32.2 (2019): 02LT01.
End 2018: From binary to ternary compounds
Inter-granular ZrO2 particles
Intra-granular ZrO2 particles
Nb
Nb3Sn with ZrO2 /HfO2
Residual core
Nb3Sn
Residual core
Nb - 4at.%Ta - 1at.%Zr
- 1at.%Hf
Sn source powders
Sn source powders + Oxide
Grain boundary
HT
HT
Internal oxidation method

## Slide 6: Why APC (ternary) Wires?
ZrO2/HfO2 nanoprecipitates or point particles (PP) as additional pinning centres (intra and inter-granular)
PP as centres of inhibition of grain growth  A-15 grain size (GS) refinement  Jc enhancement
Ta addition to raise Birr and Bc2
Alice Moros – SMP Seminar, 11th November 2021
Physics behind PP formation, size, and distribution?

## Slide 7: Microstructural Study of APC Wires
Wire recipe | T3935-675 x 380 | T3914-685 x 228 | T3912-700 x 71 | T3914-675 x 317 | T3914-700 x 120
Wire Ø [mm] | 0.84 | 0.71 | 0.71 | 0.84 | 0.71
Dopant | 4 at.% Ta, 1 at.% Zr | 4 at.% Ta, 1 at.% Hf | 4 at.% Ta, 1 at.% Zr | 4 at.% Ta, 1 at.% Hf | 4 at.% Ta, 1 at.% Hf
Heat treatment | 675 °C, 380 h | 685 °C, 228 h | 700 °C, 71 h | 675 °C, 317 h | 700 °C, 120 h
First 5 samples analyzed at TU Wien in 2020  PP size & density investigation
Other 9 samples arrived to TU Wien in 2021  size & density analyses almost completed
GS analysis ongoing
Alice Moros – SMP Seminar, 11th November 2021
Correlations between the size and density of PP and the performed HT

## Slide 8: Towards TEM Investigation
Sample preparation
FIB Lamella
Finely thinned regions are those where the hole is located
periphery
core
Alice Moros – SMP Seminar, 11th November 2021

## Slide 9: TEM Analysis – PP areas selection
Chosen Areas:
107
108
115
101
107
115
108
Area 107
Area 108
Area 115
periphery
core
FIB Lamella
Alice Moros – SMP Seminar, 11th November 2021

## Slide 10: TEM-EDX: HfO2 PP identification
Alice Moros – SMP Seminar, 11th November 2021
Atomic number
Nb3Sn = 43.25
HfO2 = 29.33
ZrO2 = 18.67
Hf M
Cu L
Cu L
Hf M

## Slide 11: TEM imaging: HfO2 vs ZrO2

## Slide 12: FIB damage in the image
PIPS refinement (with liquid nitrogen cooling) to reduce FIB damage
Alice Moros – SMP Seminar, 11th November 2021

## Slide 13
TEM Analysis HfO2 – PS & PD
High Angle Annular Dark Field – Scanning TEM for PP size analysis and EELS measurements for density evaluation
Gatan Microscopy Suite Software
HfO2
Alice Moros – SMP Seminar, 11th November 2021
Z contrast imaging

## Slide 14: Counting PP Manually
Alice Moros – SMP Seminar, 11th November 2021
Contrast, brightness, gamma adjustment for PP identification

## Slide 15: TEM Analysis ZrO2 – PS & PD
HAADF-STEM for PP size analysis and EELS measurements for density evaluation
ZrO2
Alice Moros – SMP Seminar, 11th November 2021

## Slide 16: Electron Energy Loss Spectroscopy - EELS
Alice Moros – SMP Seminar, 11th November 2021
Specimen thickness – Zero-loss peak (ZLP) and total spectrum intensity
Valence/conduction electron density – Plasmon peaks
Optical response – Low-loss distribution
Band structure and interband transitions – Near zero-loss features
Elemental composition – Core-loss edges
Bonding and oxidation state – Near edge fine structure (ELNES)
Distribution of near neighbouring atoms – Extended energy loss fine structure (ExELFS)
https://eels.info/about/overview
Scheme of the EELS system in TEM
Sample
Lenses
TEM viewing screen
Selecting aperture
Scintillator
CCD camera
Magnetic
Prism

## Slide 17: EELS for Thickness Evaluation
Alice Moros – SMP Seminar, 11th November 2021
Log-ratio formula
= Thickness
= Mean free path of the inelastic scattering (valence e-)
= Total number of e- in the EEL spectrum or total unfiltered image intensity
= The number of e- having lost no energy or zero loss peak (ZLP) intensity
Specimen thickness – Zero-loss peak (ZLP) and total spectrum intensity
https://eels.info/about/overview

## Slide 18: Elemental composition: EELS vs EDX
Alice Moros – SMP Seminar, 11th November 2021
Complementary techniques:
- EELS sensitive to lighter elements  excitation edges sharp, experimentally accessible energy losses (signal very weak beyond about 3 keV energy loss)
- EDX sensitive to heavier elements
EELS able to “fingerprint” different forms of the same element
Different energy resolution:
- ~1 eV or better for EELS
- Few tens of eV for EDX
EDX easier to use
EELS Mapping on (APC) Nb3Sn for measuring atomic composition?

## Slide 19: PS & PD – First Results
317 h
380 h
228 h
71 h
120 h
ZrO2
HfO2
ZrO2
HfO2
HfO2
No direct relationship yet between PP size + density and heat treatment parameters
HfO2
380 h
71 h
120 h
ZrO2
HfO2
HfO2
ZrO2
228 h
317 h
Alice Moros – SMP Seminar, 11th November 2021

## Slide 20: And What About GS Evaluation?
SEM Transmission Kikutchi Diffraction (TKD) or EBSD in transmission mode
Alice Moros – SMP Seminar, 11th November 2021
T3914-700 x 120 HfO2
T3912-700 x 71 ZrO2
T3914-675 x 317 HfO2

## Slide 21: GS Evaluation: SEM-TKD Analysis
Alice Moros – SMP Seminar, 11th November 2021
T3935-675 x 380 HfO2
T3914-685 x 228 HfO2
Wire recipe | T3935-675 x 380 | T3914-685 x 228 | T3912-700 x 71 | T3914-675 x 317 | T3914-700 x 120
NA [mm] | 96 ± 46 | 102 ± 76 | 73 ± 44 | 64 ± 53 | 111 ± 106
Modal value [nm] | 50 ± 5 | 55 ± 10 | 40 ± 10 | 60 ± 20 | 55 ± 10

## Slide 22: GS Evaluation: SEM-TKD Analysis
Alice Moros – SMP Seminar, 11th November 2021
Not possible to choose a precise location for GS mapping  sometimes signal is coming from very small portions
Sample preparation method and thickness uniformity
Lamella areas with unallocated points
Other techniques besides SEM-TKD?
- Fracture a wire, image the surface
Wire recipe | T3935-675 x 380 | T3914-685 x 228 | T3912-700 x 71 | T3914-675 x 317 | T3914-700 x 120
NA [mm] | 96 ± 46 | 102 ± 76 | 73 ± 44 | 64 ± 53 | 111 ± 106
Modal value [nm] | 50 ± 5 | 55 ± 10 | 40 ± 10 | 60 ± 20 | 55 ± 10
Courtesy of J. Rochester, The Ohio State University

## Slide 23: Microscopy Investigation on APC - Summary
14 samples received at TU Wien: 5 analyzed in terms of PS & PD, 9 almost completed
No direct relationship between PP size + density and heat treatment parameters so far:
Looking into completing PS & PD data with the most recently arrived samples!
SEM-TKD measurements for GS evaluation on the first 5 samples produced unreliable results: analyses still ongoing for most of the samples  how PP type and HT impact on grain refinement
Alice Moros – SMP Seminar, 11th November 2021

## Slide 24: Towards Further Exploration of APC Wires
Alice Moros – SMP Seminar, 11th November 2021
What’s behind that PD gap?
Smarter PP counting methods
PS and PD evolution at different stages for different HTs
Comparing Zr and Hf samples with same HT  changes in PD and PS
PP analysis through wire length
GS evaluation: comparison between SEM-TKD and fracture a wire
Evaluation of Sn concentration gradient according to PP type and HT performed
Other techniques besides TEM?
Small Angle Neutron Scattering (SANS)
Research is needed!
Small Angle X-ray Scattering (SAXS)
Atom Probe Tomography (ATP)

## Slide 25: Thank you for your attention!
Alice Moros – SMP Seminar, 11th November 2021
What’s behind that PD gap?
Smarter PP counting methods
PS and PD evolution at different stages for different HTs
Comparing Zr and Hf samples with same HT  changes in PD and PS
PP analysis through wire length
GS evaluation: comparison between SEM-TKD and fracture a wire
Evaluation of Sn concentration gradient according to PP type and HT performed
Other techniques besides TEM?
Small Angle Neutron Scattering (SANS)
Research is needed!
Small Angle X-ray Scattering (SAXS)
Atom Probe Tomography (ATP)