## Slide 1: Test summary for strands used in CCT3 and CCT4
D. Dietderich, D. Arbelaez, H. Higley, A. Lin, I. Pong, X. Wang
MDP Meeting
4/19/2017

## Slide 2: Strand and Cable Parameters
Strand 13695, RRP 54/61
Production year 2010
Cable 1063, 2 pass cable
April 24, 2015

## Slide 3: Metallography of cable 1063
Etched after HT

## Slide 4: LBL HD Magnet Strand Results: RRP 54/61, 0.80 mm diameter, ~50% Cu
RRP 60/61

## Slide 5: MJR 54/61: Stability Current for vs. RRR of wire
MJR & RRP
Internal Tin

## Slide 6: RRR data
77 K data for the extracted strand
CCT3 Witness Round wire RRR
High temperature step: 650-660C for 48 hrs

## Slide 7: Relation between RRR vs. Rr (77 K)

## Slide 8: Extracted strands preparation
Nb3Sn RRP 54/61
      0.8 mm diameter before heat treatment,
      non-Cu fraction 54%
Samples extracted from cable #1063
  Extracted wires straightened before being wound on to Ti-alloy barrels
Different heat treatments dates:
      Peak temperature of 650-660 C for 48 hrs.
After soldering wires to barrels the samples were cleaned with soap solution in ultrasonic bath
Stycast or solder flux was applied to secure the wires to the barrels
Voltage taps were installed on to wires after the Stycast was applied and cured.

## Slide 9: Typical heat treatment rack with samples installed
Andy Lin

## Slide 10: Sample 4 – second one burned up at the bell/barrel transition

## Slide 11: Round Strand: Stable at 1200 A and below from ramps from 0 to 10 T
conductor load line
Ic(4.2K)
quench current
I and B range for the sweep
Strands in cable 1063
PS limit

## Slide 12: Extracted Strand HT’ed with CCT3: Stable at 1000 A from 0 to 10 T
Extracted strand From cable 1063
No field sweeps done above 1,000 A

## Slide 13: Extracted Strand: Stable below 1200 A from 0 to 10 T
Extracted strand From cable 1063
conductor load line
Ic (4.2 K)
quench current
I and B range for the sweep
PS limit
Quench current was measured by increasing the current during the down ramp of the magnetic field
Conductor load line was calculated by L. Brouwer considering the iron