## Slide 1
S. Viarengo1,2, P. Ferracin2, Laura Savoldi1, Fabio Freschi1, X. Wang2, L. Brouwer2
1Politecnico di Torino, Torino, Italy
2Lawrence Berkeley National Lab, Berkeley, CA
MDP Collaboration Meeting, Virtual, 5/17/2022
Multiphysics modeling for REBCO CORC cables based on T-A formulation

## Slide 2: Outline
Framework
Activity objective
Tape modeling
  REBCO design
  Critical current density evaluation
  Mathematical model
  Model setup, geometry and mesh
  Results
CORC modeling
  VPI test in LBL
  Cable design
  2D model
  Full 3D model ongoing
Next steps
References

## Slide 3: Framework
REBCO CORC cable for CCT application
[Status of CORC® cables and wires for use in highfield magnets and power systems a decade after their introduction, D.C. Van der Laan et al, 2019]
C2 wire layout
(Courtesy of LBL)

## Slide 4: Activity objective: multi-scale approach
Jc characterization of a homogenous material for the single tape
Validation on a straigth Conductor on Round Core Cable (CORC)
Validation on a bended CORC
Scaling up to the CCT: development of an equivalent model based on AI?

## Slide 5: Tape modeling

## Slide 6: REBCO Tape design
Thermal-physical properties as function of temperature θ and RRR
λ, ρ weigthed on the cross section and cp on the mass
Rcu
Rsilver
Rsubstrate
RYBCO
Rcu
Rsilver
i
icu
icu
isilver
iYBCO
isub
isilver
Copper stabilizer
20 μm
REBCO
1.6 μm
Buffer zone
0.4 μm
Substrate
50 μm
Silver layer
1.6 μm
2.2 mm
95.2 μm
Power Law
SCS-4050 by SuperPower 2008
[Two-Dimensional Anisotropic Model of YBCO Coated Conductors, Casali et. al, 2015]
[In-Field Electrical Resistance at 4.2 K of REBCO Splices, J. Fleiter and A. Ballarino, et. al, 2017]
y
density

## Slide 7: Critical current density
Parameter | Value | Unit
* |  | 
Parameter | Value | Unit
* At 4.2 K.
[Performance correlation between YBa2Cu3O7-δ coils and short samples for coil technology development, X. Wang et. al, 2016]
[Self-Consistent Modeling of the Ic of HTS Devices: How Accurate do Models Really Need to Be?, Grilli et. al, 2014]

## Slide 8: Mathematical model (1)
Governing equations:
  T-formulation (Tape)
  A-formulation (Air)
Thin shell approximation:
Joule losses from T-formulation!
REBCO tape
Air domain
  Heat conduction equation (Tape)
[Study of magnetization loss of CORC cables using 3D T-A formulation, Y. Wang, 2019]
[3D quench modeling base on T-A formulation for high temperature superconductor CORC cables, Y. Wang, 2019]

## Slide 9: Mathematical model (2)
y
x
z
T
Jz
Jy=0
Jx=0
Jz
T
Final governing equation:
n

## Slide 10: Model set up
Injection of a ramp of current on the tape cross section
Tape immersed in a bath of liquid nitrogen @ 77 K
External field applied
2D/3D simulations
REBCO tape
Air domain

## Slide 11: Geometry and mesh
Air domain: tetrahedral mesh
Tape domain: triangular mesh
Elements in tape width: 100
N° cells: ~60,000

## Slide 12: Model validation @ 4.2 K
Bapp (T) | N-value | Errn-value (%) | Errav,V (%)
0.4 | 45 | 6% | 7%
0.7 | 40 | 6% | 6%
1 | 32 | 0% | 3%
2 | 45 | 1% | 4%
4 | 37 | 7% | 8%
7 | 35 | 9% | 9%
10 | 45 | 3% | 5%
12 | 32 | 0% | 2%
13 | 40 | 1% | 3%
15 | 40 | 18% | 10%

## Slide 13: Results : self-field at @ 77 K
Good agreement on V-I characteristic

## Slide 14: Results: vertical field applied at @ 77 K
Wrt 4.2 K
Strong Ic degradation
Lower n-value: 30-25

## Slide 15: CORC modeling

## Slide 16: VPI test in LBNL
[Developing a Vacuum Pressure Impregnation Procedure for CORC® Wires, J. Sterne et. al, MT27, 2021]
[Distributed fiber optic sensing to identify locations of resistive transitions in REBCO conductors and magnets, L. Luo et. al, MT27 2021]
3 layers
2 REBCO tapes/layer (6 tapes total)
2.9 mm diameter
Bending radii: 20 – 50 mm
3 set of experiments:
  Set 1: straigth CORC cable, before bending
  Set 2: bended CORC cable, before epoxy impregnation
  Set 3: bended CORC cable, after epoxy impregnation

## Slide 17: Cable layout
Din
pitch
Copper stabilizer
5 μm
REBCO
1.6 μm
Buffer zone
0.4 μm
Substrate
30 μm
Silver layer
1.6 μm
2.02 mm
45.2 μm
Parameter | Value | Unit
Parameter | Value | Unit

## Slide 18: Geometry and mesh
2D cross section
Triangular mesh
Elements per tape: 100 - 200
N° cells: 13,000

## Slide 19: Model set up
Temperature imposed @ 77 K
Purely resistive flow
No current sharing between layers
Equivalent electric network:

## Slide 20: Results (1): self-field at @ 77 K
Rigth direction

## Slide 21: Improvements (1)
Thermal model
Free convection
y

## Slide 22: Improvements (2)
Electromagnetic model
Weak form T-A formulation:
[Calculations of the AC losses in superconducting cables and coils: Neumann boundary conditions of T-A formulation. S. Wang, 2022]
New BC!
Current injection weak constraint!

## Slide 23: Next steps
Complete full 3D model
Thermal and electromagnetic model improvements
3D model of bended CORC cable (before\after epoxy)
Modeling more layers and tapes

## Slide 24: References
Status of CORC® cables and wires for use in highfield magnets and power systems a decade after their introduction, D.C. Van der Laan et al, 2019
Two-Dimensional Anisotropic Model of YBCO Coated Conductors, Casali et. al, 2015
In-Field Electrical Resistance at 4.2 K of REBCO Splices, J. Fleiter and A. Ballarino, et. al, 2017
Self-Consistent Modeling of the Ic of HTS Devices: How Accurate do Models Really Need to Be?, Grilli et. al, 2014
Performance correlation between YBa2Cu3O7-δ coils and short samples for coil technology development, X. Wang et. al, 2016
Study of magnetization loss of CORC cables using 3D T-A formulation, Y. Wang, 2019
3D quench modeling base on T-A formulation for high temperature superconductor CORC cables, Y. Wang, 2019
Developing a Vacuum Pressure Impregnation Procedure for CORC® Wires, J. Sterne et. al, MT27, 2021
Distributed fiber optic sensing to identify locations of resistive transitions in REBCO conductors and magnets, L. Luo et. al, MT27 2021
Calculations of the AC losses in superconducting cables and coils: Neumann boundary conditions of T-A formulation, S. Wang, 2022