## Slide 1: Unit 13-14 Electro-magnetic forces and stresses in superconducting accelerator magnets
Paolo Ferracin
Lawrence Berkeley National Laboratory (LBNL)
Maxim Marchevsky
Lawrence Berkeley National Laboratory (LBNL)
Ezio Todesco
European Organization for Nuclear Research (CERN)

## Slide 2: Outline
Introduction
Electro-magnetic force
  Definition and directions
Magnetic pressure and forces
Approximations of practical winding cross-sections
  Thin shell, Thick shell, Sector
Stored energy and end forces
Stress and strain
Pre-stress
Conclusions

## Slide 3: References
[1] Y. Iwasa, “Case studies in superconducting magnets”, New York, Plenum Press, 1994.
[2] M. Wilson, “Superconducting magnets”, Oxford UK: Clarendon Press, 1983.
[3] A.V. Tollestrup, “Superconducting magnet technology for accelerators”, Ann. Reo. Nucl. Part. Sci. 1984. 34, 247-84.
[4] K. Koepke, et al., “Fermilab doubler magnet design and fabrication techniques”, IEEE Trans. Magn., Vol. MAG-15, No. l, January 1979.
[5] S. Wolff, “Superconducting magnet design”, AIP Conference Proceedings 249, edited by M. Month and M. Dienes, 1992, pp. 1160-1197.
[6] A. Devred, “The mechanics of SSC dipole magnet prototypes”, AIP Conference Proceedings 249, edited by M. Month and M. Dienes, 1992, p. 1309-1372.
[7] T. Ogitsu, et al., “Mechanical performance of 5-cm-aperture, 15-m- long SSC dipole magnet prototypes”, IEEE Trans. Appl. Supercond., Vol. 3, No. l, March 1993, p. 686-691.
[8] J. Muratore, BNL, private communications.
[9] “LHC design report v.1: the main LHC ring”, CERN-2004-003-v-1, 2004.
[10]A.V. Tollestrup, “Care and training in superconducting magnets”, IEEE Trans. Magn.,Vol. MAGN-17, No. l, January 1981, p. 863-872.
[11] N. Andreev, K. Artoos, E. Casarejos, T. Kurtyka, C. Rathjen, D. Perini, N. Siegel, D. Tommasini, I. Vanenkov, MT 15 (1997) LHC PR 179.
[12]E. Todesco, “Masterclass - Design of superconducting magnets for particle accelerators”, https://indico.cern.ch/category/12408/

## Slide 4: 1. Introduction
Superconducting accelerator magnets are characterized by high fields and high current densities.
As a results, the coil is subjected to strong electro-magnetic forces, which tend to move the conductor and deform the winding.
A good knowledge of the magnitude and direction of the electro-magnetic forces, as well as of the stress of the coil, is mandatory for the mechanical design of a superconducting magnet.
In this unit we will describe the effect of these forces on the coil through simplified approximation of practical winding, and we will introduced the concept of pre-stress, as a way to mitigate their impact on magnet performance.

## Slide 5: 2. Electro-magnetic force Definition
In the presence of a magnetic field (induction) B, an electric charged particle q in motion with a velocity v is acted on by a force FL called electro-magnetic (Lorentz) force [N]:
A conductor element carrying current density J (A/mm2) is subjected to a force density fL [N/m3]
The e.m. force acting on a coil is a body force, i.e. a force that acts on all the portions of the coil (like the gravitational force).

## Slide 6: 2. Electro-magnetic force Dipole magnets
Main field components is By
  Perpendicular to the axis of the magnet z
Electro-magnets: field produced by a current (or current density)
Magnetic field steers (bends) the particles in a circular orbit
by E. Todesco



## Slide 7: 2. Electro-magnetic force Quadrupole magnet
The force necessary to stabilize linear motion is provided by the quadrupoles
  They provide a field
    equal to zero in the center
    increasing linearly with the radius
They act as a spring: focus the beam
Prevent protons from falling to the bottom of the aperture due to the gravitational force
  it would happen in less than 60 ms
by E. Todesco



## Slide 8: 2. Electro-magnetic force Quadrupole magnets
A typical accelerator structure is the FODO cell
  Alternating quadrupoles spaced by length L of similar gradient
One can prove that this gives positive focusing in both transverse planes




by E. Todesco

## Slide 9: 2. Electro-magnetic force Definition
The superconducting coil (with a J) is in its own field B

## Slide 10: 2. Electro-magnetic force Dipole magnets
The e.m. forces in a dipole magnet tend to push the coil
  Towards the mid-plane in the vertical-azimuthal direction (Fy, F < 0)
  Outwards in the radial-horizontal direction (Fx, Fr > 0)
Tevatron dipole
HD2

## Slide 11: 2. Electro-magnetic force Quadrupole magnets
The e.m. forces in a quadrupole magnet tend to push the coil
  Towards the mid-plane in the vertical-azimuthal direction (Fy, F < 0)
  Outwards in the radial-horizontal direction (Fx, Fr > 0)
TQ
HQ

## Slide 12: 2. Electro-magnetic force End forces in dipole and quadrupole magnets
In the coil ends the Lorentz forces tend to push the coil
  Outwards in the longitudinal direction (Fz > 0)
Similarly as for the solenoid, the axial force produces an axial tension in the coil straight section.

## Slide 13: 2. Electro-magnetic force End forces in dipole and quadrupole magnets
Nb-Ti LHC MB (values per aperture)
  Fx = 340 t per meter
    ~300 compact cars
    Precision of coil positioning: 20-50 μm
  Fz = 27 t
    ~weight of the cold mass
Nb3Sn dipole (HD2)
  Fx = 500 t per meter
  Fz = 85 t
  These forces are applied to an objet with a cross-section of 150x100 mm !!!
    and by the way, it is brittle

## Slide 14: 2. Electro-magnetic force Solenoids
The e.m. forces in a solenoid tend to push the coil
  Outwards in the radial-direction (Fr > 0)
  Towards the mid plane in the vertical direction (Fy < 0)
Important difference between solenoids and dipole/quadrupole magnets
  In a dipole/quadrupole magnet the horizontal component pushes outwardly the coil
    The force must be transferred to a support structure
  In a solenoid the radial force produces a circumferential hoop stress in the winding
    The conductor, in principle, could support the forces with a reacting tension

## Slide 15: Outline
Introduction
Electro-magnetic force
  Definition and directions
Magnetic pressure and forces
Approximations of practical winding cross-sections
  Thin shell, Thick shell, Sector
Stored energy and end forces
Stress and strain
Pre-stress
Conclusions

## Slide 16: 3. Magnetic pressure and forces
The magnetic field is acting on the coil as a pressurized gas on its container.
Let’s consider the ideal case of a infinitely long “thin-walled” solenoid, with thickness d, radius a, and current density Jθ .
The field outside the solenoid is zero. The field inside the solenoid B0 is uniform, directed along the solenoid axis and given by
The field inside the winding decreases linearly from B0 at a to zero at a + . The average field on the conductor element is B0/2, and the resulting Lorentz force is radial and given by

## Slide 17: 3. Magnetic pressure and forces
We can therefore define a magnetic pressure pm acting on the winding surface element:
where
So, with a 10 T magnet, the windings undergo a pressure pm = (102)/(2· 4   10-7) = 4  107 Pa = 390 atm.
The force pressure increase with the square of the field.
A pressure [N/m2] is equivalent to an energy density [J/m3].

## Slide 18: Outline
Introduction
Electro-magnetic force
  Definition and directions
Magnetic pressure and forces
Approximations of practical winding cross-sections
  Thin shell, Thick shell, Sector
Stored energy and end forces
Stress and strain
Pre-stress
Conclusions

## Slide 19: 4. Approximations of practical winding cross-sections
In order to estimate the force, let’s consider three different approximations for a n-order magnet
  Thin shell (see Appendix I)
    Current density J = J0 cosn (A per unit circumference) on a infinitely thin shell
      Orders of magnitude and proportionalities
  Thick shell (see Appendix II)
    Current density J = J0 cosn (A per unit area) on a shell with a finite thickness
      First order estimate of forces and stress
  Sector (see Appendix III)
    Current density J = const (A per unit area) on a a sector with a maximum angle  = 60º/30º for a dipole/quadrupole
      First order estimate of forces and stress

## Slide 20: 4. Approximations of practical winding cross-sections: thin shell
We assume
  J = J0 cosn where J0 [A/m] is ⊥ to the cross-section plane
  Radius of the shell/coil = a
  No iron
The field inside the aperture is
The average field in the coil is
The Lorentz force acting on the coil [N/m2] is

## Slide 21: 4. Approximations of practical winding cross-sections: thin shell (dipole)
In a dipole, the field inside the coil is
The total force acting on the coil [N/m] is
The Lorentz force on a dipole coil varies
  with the square of the bore field
  linearly with the magnetic pressure
  linearly with the bore radius.
In a rigid structure, the force determines an azimuthal displacement of the coil and creates a separation at the pole.
The structure sees Fx.

## Slide 22: 4. Approximations of practical winding cross-sections: thin shell (quadrupole)
In a quadrupole, the gradient [T/m] inside the coil is
The total force acting on the coil [N/m] is
The Lorentz force on a quadrupole coil varies
  with the square of the gradient or coil peak field
  with the cube of the aperture radius (for a fixed gradient).
Keeping the peak field constant, the force is proportional to the aperture.

## Slide 23: 4. Approximations of practical winding cross-sections: thick shell
If we assume
  J = J0 cos where J0 [A/m2] is  to the cross-section plane
  Inner (outer) radius of the coils = a1 (a2)
The generated field is a pure dipole
Linear dependence on coil width
Easier to achieve with a Rutherford cable

## Slide 24: 4. Approximations of practical winding cross-sections: thick shell
We assume
  J = J0 cosn where J0 [A/m2] is ⊥ to the cross-section plane
  Inner (outer) radius of the coils = a1 (a2)
  No iron
The field inside the aperture is
The field in the coil is
The Lorentz force acting on the coil [N/m3] is

## Slide 25: 4. Approximations of practical winding cross-sections: sector (dipole)
We assume
  J=J0 is ⊥ the cross-section plane
  Inner (outer) radius of the coils = a1 (a2)
  Angle  = 60º (third harmonic term is null)
  No iron
The field inside the aperture
The field in the coil is

## Slide 26: 4. Approximations of practical winding cross-sections: comparison

## Slide 27: Outline
Introduction
Electro-magnetic force
  Definition and directions
Magnetic pressure and forces
Approximations of practical winding cross-sections
  Thin shell, Thick shell, Sector
Stored energy and end forces
Stress and strain
Pre-stress
Conclusions

## Slide 28: 5. Stored energy and end forces
The magnetic field possesses an energy density [J/m3]
The total energy [J] is given by
Or, considering only the coil volume, by
Knowing the inductance L, it can also be expresses as
The total energy stored is strongly related to mechanical and protection issues.

## Slide 29: 5. Stored energy and end forces
The stored energy can be used to evaluate the Lorentz forces. In fact
This means that, considering a “long” magnet, one can compute the end force Fz [N] from the stored energy per unit length W [J/m]:
where AZ is the vector potential, given by

## Slide 30: 5. Stored energy and end forces Thin shell
For a dipole, the vector potential within the thin shell is
and, therefore,
  The axial force on a dipole coil varies
    with the square of the bore field
    linearly with the magnetic pressure
    with the square of the bore radius.
For a quadrupole, the vector potential within the thin shell is
and, therefore,
  Being the peak field the same, a quadrupole has half the Fz of a dipole.

## Slide 31: Outline
Introduction
Electro-magnetic force
  Definition and directions
Magnetic pressure and forces
Approximations of practical winding cross-sections
  Thin shell, Thick shell, Sector
Stored energy and end forces
Stress and strain
Pre-stress
Conclusions

## Slide 32: 6. Stress and strain Definitions
A stress  or  [Pa] is an internal distribution of force [N] per unit area [m2].
  When the forces are perpendicular to the plane the stress is called normal stress () ; when the forces are parallel to the plane the stress is called shear stress ().
  Stresses can be seen as way of a body to resist the action (compression, tension, sliding) of an external force.
A strain  (l/l0) is a forced change dimension l of a body whose initial dimension is l0.
  A stretch or a shortening are respectively a tensile or compressive strain; an angular distortion is a shear strain.

## Slide 33: 6. Stress and strain Definitions
The elastic modulus (or Young modulus, or modulus of elasticity) E [Pa] is a parameter that defines the stiffness of a given material. It can be expressed as the rate of change in stress with respect to strain (Hook’s law):
 =  /E
The Poisson’s ratio  is the ratio between “axial” to “transversal” strain. When a body is compressed in one direction, it tends to elongate in the other direction. Vice versa, when a body is elongated in one direction, it tends to get thinner in the other direction.
 = -axial/ trans

## Slide 34: 6. Stress and strain Definitions
By combining the previous definitions, for a biaxial stress state we get
and
Compressive stress is negative, tensile stress is positive.
The Poisson’s ration couples the two directions
  A stress/strain in x also has an effect in y.
For a given stress, the higher the elastic modulus, the smaller the strain and displacement.

## Slide 35: 6. Stress and strain Failure/yield criteria
The proportionality between stress and strain is more complicated than the Hook’s law
  A: limit of proportionality (Hook’s law)
  B: yield point
    Permanent deformation of 0.2 %
  C: ultimate strength
  D: fracture point
Several failure criteria are defined to estimate the failure/yield of structural components, as
  Equivalent (Von Mises) stress v  yield , where



## Slide 36: 6. Stress and strain Mechanical properties
Superconducting coil Nb-Ti: non trivial to characterize, since it is non linear and has hysteresis
Stress-strain relation for Nb-Ti coil of the HL-LHC D1 dipole (M. Sugano, et al.)

## Slide 37: 6. Stress and strain Mechanical properties
Superconducting coil Nb3Sn
  Also in this case, since it is non linear and has hysteresis
  The coil is harder since it is impregnated (20-40 GPa)
  The coil has a definite size at 0 MPa, contrary to Nb-Ti
Stress-strain for Nb3Sn cable (G. Vallone)

## Slide 38: 6. Stress and strain Mechanical properties
Superconducting coil Nb3Sn
  A degradation of performance is seen around 150-200 MPa
Degradation of critical current for Nb3Sn cable (J. Fleiter)

## Slide 39: 6. Stress and strain Mechanical design principles
The e.m forces push the conductor towards mid-planes and supporting structure.
The resulting strain is an indication of
  a change in coil shape
    effect on field quality
  a displacement of the conductor
    potential release of frictional energy and consequent quench of the magnet
The resulting stress must be carefully monitored
  In Nb-Ti magnets, possible damage of kapton insulation at about 150-200 MPa.
  In Nb3Sn magnets, possible conductor degradation at about 150-200 MPa.
  In general, al the components of the support structure must not exceed the stress limits.
Mechanical design has to address all these issues.

## Slide 40: 6. Stress and strain Mechanical design principles
LHC dipole at 0 T LHC dipole at 9 T
Usually, in a dipole or quadrupole magnet, the highest stresses are reached at the mid-plane, where all the azimuthal e.m. forces accumulate (over a small area).
Displacement scaling = 50

## Slide 41: 6. Stress and strain Thick shell
For a dipole,
For a quadrupole,
No shear

## Slide 42: 6. Stress and strain A practical example: 20 T hybrid dipole
Nb3Sn and Bi2212 cross at 14.5 T at 4.2 K and 16.5 T at 1.9 K

## Slide 43: 6. Stress and strain A practical example: 20 T hybrid dipole
50 mm aperture
ID Nb3Sn = 146 mm
OD Nb3Sn = 200 mm
76 m total coil thickness
  49 mm thick Bi2212 coil
  27 mm thick Nb3Sn coil
Area Bi2212: 2540 mm2 (1 quadrant)
Area Nb3Sn: 2470 mm2 (1 quadrant)
Stored energy: 2.86 MJ/m (4 quadrants)
20 T = 13 T + 7 T
Bi2212
Nb3Sn

## Slide 44: 6. Stress and strain A practical example: 20 T hybrid dipole
Bi2212
Nb3Sn
Bi2212
Bi2212
Nb3Sn
ID: 50 mm
OD: 146 mm
W: 49 mm
ID: 146 mm
OD: 200 mm
W: 27 mm
ID: 50 mm
OD: 200 mm
W: 76 mm

## Slide 45: 6. Stress and strain A practical example: 20 T hybrid dipole
Operation Je  coil size  azimuthal and radial stresses

## Slide 46: Summary
We need to build a
  13-14 T HTS magnet (50 mm)
  10-13 T LTS magnet (large bore)
    120 mm seems a good start, but we may need more
In hybrid 20 T, radial stress seems higher than azimuthal
  When tested separately, very high azimuthal stress in LTS
ID: 50 mm
OD: 146 mm
W: 49 mm
B_bore_op = 14.7 T
/ r =128/122
ID: 146 mm
OD: 200 mm
W: 27 mm
B_bore_op = 10.3 T
/ r =232/77
ID: 50 mm
OD: 200 mm
W: 76 mm
B_bore_op = 20 T
/ r =188/206

## Slide 47: 6. Stress and strain Azimuthal vs radial stress
Azimuthal stress
  Accumulation of stress on the edge of the coil of the azimuthal component
The midplane stress at the edge is
  Proportional to current density
  Proportional to field
  Proportional to aperture radius
by E. Todesco

## Slide 48: 6. Stress and strain Azimuthal vs radial stress
Radial stress
  For the radial stress, we have to integrate along the midplane
  This equation can be rewritten, ignoring the iron contribution, in a form where the magnetic pressure is put in evidence: for a sector coil one has
by E. Todesco

## Slide 49: 6. Stress and strain Azimuthal vs radial stress
Azimuthal stress
  Can be cured by lower current density to get higher fields
  Pay attention to the aperture
Radial stress
  Not much you can do when you get to very high field
    (stress management)
by E. Todesco

## Slide 50: Outline
Introduction
Electro-magnetic force
  Definition and directions
Magnetic pressure and forces
Approximations of practical winding cross-sections
  Thin shell, Thick shell, Sector
Stored energy and end forces
Stress and strain
Pre-stress
Conclusions

## Slide 51: 7. Pre-stress
A.V. Tollestrup, [3]

## Slide 52: 7. Pre-stress Tevatron main dipole
Let’s consider the case of the Tevatron main dipole (Bnom= 4.4 T).
In a infinitely rigid structure without pre-stress the pole would move of about -100 m, with a stress on the mid-plane of -45 MPa.

## Slide 53: 7. Pre-stress Tevatron main dipole
We can plot the displacement and the stress along a path moving from the mid-plane to the pole.
In the case of no pre-stress, the displacement of the pole during excitation is about -100 m.

## Slide 54: 7. Pre-stress Tevatron main dipole
We now apply to the coil a pre-stress of about -33 MPa, so that no separation occurs at the pole region.
The displacement at the pole during excitation is now negligible, and, within the coil, the conductors move at most of -20 m.

## Slide 55: 7. Pre-stress Tevatron main dipole
We focus now on the stress and displacement of the pole turn (high field region) in different pre-stress conditions.
The total displacement of the pole turn is proportional to the pre-stress.
  A full pre-stress condition minimizes the displacements.

## Slide 56: No pre-stress, no e.m. force
Displacement scaling = 50

## Slide 57: No pre-stress, with e.m. force
Displacement scaling = 50
About 100 μm for Tevatron main dipole (Bnom= 4.4 T)

## Slide 58: Pre-stress, no e.m. force
Pole shim
Displacement scaling = 50

## Slide 59: Pre-stress, with e.m. force
Pole shim
Displacement scaling = 50
Coil pre-stress applied to all the accelerator dipole magnets

## Slide 60: 7. Pre-stress Overview of accelerator dipole magnets
The practice of pre-stressing the coil has been applied to all the accelerator dipole magnets
  Tevatron [4]
  HERA [5]
  SSC [6]-[7]
  RHIC [8]
  LHC [9]
The pre-stress is chosen in such a way that the coil remains in contact with the pole at nominal field, sometime with a “mechanical margin” of more than 20 MPa.

## Slide 61: 7. Pre-stress General considerations
As we pointed out, the pre-stress reduces the coil motion during excitation.
This ensure that the coil boundaries will not change as we ramp the field, and, as a results, minor field quality perturbations will occur.
What about the effect of pre-stress on quench performance?
  In principle less motion means less frictional energy dissipation or resin fracture.
  Nevertheless the impact of pre-stress on quench initiation remains controversial

## Slide 62: 7. Pre-stress General considerations
The paradigm is still used today, requiring no detachment of the coil at nominal current
  On the other hand there are several examples magnets operating with pole detachment
The paradigm is always used in design and not always followed in reality
  Typically, for the first models and prototypes one speaks of “conservative” loading, meaning that the preload is lower than what required to avoid pole unloading in operational conditions
  The fear is to break something of degrade the conductor

## Slide 63: 7. Pre-stress Experience in Tevatron
  Above movements of 0.1 mm, there is a correlation between performance and movement: the larger the movement, the longer the training
  Conclusion: one has to pre-stress to avoid movements that can limit performance
0.1 mm
A.V. Tollestrup, [10]

## Slide 64: 7. Pre-stress Experience in LHC short dipoles
Study of variation of pre-stress in several models – evidence of unloading at 75% of nominal, but no quench
“It is worth pointing out that, in spite of the complete unloading of the inner layer at low currents, both low pre-stress magnets showed correct performance and quenched only at much higher fields”
N. Andreev, [11]

## Slide 65: 7. Pre-stress Experience in LARP TQ quadrupole
With low pre-stress, unloading but still good quench performance
With high pre-stress, stable plateau but small degradation
TQS03b high prestress
TQS03a low prestress
TQS03a low prestress
TQS03b high prestress

## Slide 66: 7. Pre-stress Experience in MQXFS quadrupole
“The experiment proves that (i) a preload to 60% of short sample allows operating the magnet at 85% of short sample without significant training and (ii) a preload at 80% of short sample allows to expand the operational field of the magnet from 90% to 95% of short sample current, and to reduce the training.”

## Slide 67: 8. Conclusions
We presented the force profiles in superconducting magnets
  A solenoid case can be well represented as a pressure vessel
  In dipole and quadrupole magnets, the forces are directed towards the mid-plane and outwardly.
    They tend to separate the coil from the pole and compress the mid-plane region
    Axially they tend to stretch the windings
We provided a series of analytical formulas to determine in first approximation forces and stresses.
The importance of the coil pre-stress has been pointed out, as a technique to minimize the conductor motion during excitation.

## Slide 68: Appendix I Thin shell approximation

## Slide 69: Appendix I: thin shell approximation Field and forces: general case
We assume
  J = J0 cosn where J0 [A/m] is  to the cross-section plane
  Radius of the shell/coil = a
  No iron
The field inside the aperture is
The average field in the coil is
The Lorentz force acting on the coil [N/m2] is

## Slide 70: Appendix I: thin shell approximation Field and forces: dipole
In a dipole, the field inside the coil is
The total force acting on the coil [N/m] is
The Lorentz force on a dipole coil varies
  with the square of the bore field
  linearly with the magnetic pressure
  linearly with the bore radius.
In a rigid structure, the force determines an azimuthal displacement of the coil and creates a separation at the pole.
The structure sees Fx.

## Slide 71: Appendix I: thin shell approximation Field and forces: quadrupole
In a quadrupole, the gradient [T/m] inside the coil is
The total force acting on the coil [N/m] is
The Lorentz force on a quadrupole coil varies
  with the square of the gradient or coil peak field
  with the cube of the aperture radius (for a fixed gradient).
Keeping the peak field constant, the force is proportional to the aperture.

## Slide 72: Appendix I: thin shell approximation Stored energy and end forces: dipole and quadrupole
For a dipole, the vector potential within the thin shell is
and, therefore,
  The axial force on a dipole coil varies
    with the square of the bore field
    linearly with the magnetic pressure
    with the square of the bore radius.
For a quadrupole, the vector potential within the thin shell is
and, therefore,
  Being the peak field the same, a quadrupole has half the Fz of a dipole.

## Slide 73: Appendix I: thin shell approximation Total force on the mid-plane: dipole and quadrupole
If we assume a “roman arch” condition, where all the fθ accumulates on the mid-plane, we can compute a total force transmitted on the mid-plane Fθ [N/m]
For a dipole,
For a quadrupole,
  Being the peak field the same, a quadrupole has half the Fθ of a dipole.
  Keeping the peak field constant, the force is proportional to the aperture.

## Slide 74: Appendix II Thick shell approximation

## Slide 75: Appendix II: thick shell approximation Field and forces: general case
We assume
  J = J0 cosn where J0 [A/m2] is  to the cross-section plane
  Inner (outer) radius of the coils = a1 (a2)
  No iron
The field inside the aperture is
The field in the coil is
The Lorentz force acting on the coil [N/m3] is

## Slide 76: Appendix II: thick shell approximation Field and forces: dipole
In a dipole, the field inside the coil is
The total force acting on the coil [N/m] is

## Slide 77: Appendix II: thick shell approximation Field and forces: quadrupole
In a quadrupole, the field inside the coil is
being
The total force acting on the coil [N/m] is

## Slide 78: Appendix II: thick shell approximation Stored energy, end forces: dipole and quadrupole
For a dipole,
and, therefore,
For a quadrupole,
and, therefore,

## Slide 79: Appendix II: thick shell approximation Stress on the mid-plane: dipole and quadrupole
For a dipole,
For a quadrupole,
No shear

## Slide 80: Appendix III Sector approximation

## Slide 81: Appendix III: sector approximation Field and forces: dipole
We assume
  J=J0 is  the cross-section plane
  Inner (outer) radius of the coils = a1 (a2)
  Angle  = 60º (third harmonic term is null)
  No iron
The field inside the aperture
The field in the coil is

## Slide 82: Appendix III: sector approximation Field and forces: dipole
The Lorentz force acting on the coil [N/m3], considering the basic term, is
The total force acting on the coil [N/m] is

## Slide 83: Appendix III: sector approximation Field and forces: quadrupole
We assume
  J=J0 is  the cross-section plane
  Inner (outer) radius of the coils = a1 (a2)
  Angle  = 30º (third harmonic term is null)
  No iron
The field inside the aperture
The field in the coil is

## Slide 84: Appendix III: sector approximation Field and forces: quadrupole
The Lorentz force acting on the coil [N/m3], considering the basic term, is
The total force acting on the coil [N/m] per octant is

## Slide 85: Appendix III: sector approximation Stored energy, end forces: dipole and quadrupole
For a dipole,
and, therefore,
For a quadrupole,
and, therefore,

## Slide 86: Appendix III: sector approximation Stress on the mid-plane: dipole and quadrupole
For a dipole,
For a quadrupole,
No shear